| BO-COAX RG06 AU-ZH 75 OHM DOUBLE SCREENED 75 OHM RF COAXIAL CABLE |  |
| --- | --- |

Image for illustration only

| (A) INNER CONDUCTOR | COPPERWELD | ø 0,72 |
| --- | --- | --- |
| (B) DIELECTRIC | LOW DENSITY POLYETHYLENE | ø 4,70 ± 0,10 mm |
| (C) 1° BRAID | SILVERED COPPER - COVERAGE | 168 x 0,13 mm 97% |
| (D) 2° BRAID | PLAIN COPPER - COVERAGE | 168 x 0,13 mm 95% |
| (E) NON-MIGRATING | POLYESTER TAPE | h. 20 mm |
| (F) SHEATH - COLOUR - PRINTING | FLAME RETARDANT NON-CORROSIVE THERMOPLASTIC FREE OF HALOGENS - BLACK - RAL 9004 - Standard | ø 8,50 ± 0,10 mm |
| Technical Data | Minimum Bending Radius (mm): - Singel - Repeated Temparature Range: Cable Weight (Kg/Km): - Copper - Plastic - Total | ø EXTERNAL X 5 ø EXTERNAL X 10 -40 °C / +80 °C 50,5 63,9 114,4 |
| Electrical Data (ELECTRICAL PROPERTIES at 20°C) | Impedance: Capacitance: Velocity Ratio: Resistance: - Inner Conductor - Braid Tension: - Sheath Spark Testing | 75 ± 3 Ohm 67 pF/m 66% 97 Ohm/Km 5 Ohm/Km 7,0 kV |

The producer reserves himself to make modification on the item without any notice